## Slide 1
MIL125 original cif (PBE optimized / from github)
Method
github에서 수집
https://github.com/WMD-group/Crystal_structures/blob/master/MOFs/MIL-125/2010_PBE/MIL125.cif
VESTA에서 시각화

## Slide 2
MIL125 primitive cell cif (PBE optimized / transformed with pymatgen script)
2x2x2 Supercell
Primitive Cell
Method
jupyter notebook 에서 python 라이브러리 pymatgen을 사용해 standard primitive cell로 변환
https://github.com/dydtkddl/PSID_server_room/blob/main/qe/%5B00%5DBAMOF/01ori_coordinate/primitive.ipynb
VESTA에서 시각화
VESTA에서 2x2x2 boundary 확장 및 슈퍼셀 시각화

## Slide 3
MIL125-NH2 primitive cell cif ( NH2 added by Avogadro program and pymatgen script)
2x2x2 Supercell
Primitive Cell
Method
Avogadro Program을 사용해서 NH2로 바꿀 H의 원자이름:원자번호 추출 및 VScode 상에서 해당 원자를 Nitrogen으로 변경
N원자를 기준으로 가장 가까운 C로부터 N으로 향하는 방향벡터를 이용 N에서부터 해당 벡터를 뻗고 SP3 각도를 가지도록 H두개를 적절한 위치 (N과의 거리 약 1.3 A)에 배치하는 스크립트 작성 이후 Pymatgen으로 cif로 변환
https://github.com/dydtkddl/PSID_server_room/blob/main/qe/%5B00%5DBAMOF/01ori_coordinate/primitive.ipynb
VESTA에서 시각화
VESTA에서 2x2x2 boundary 확장 및 슈퍼셀 시각화

## Slide 4
BAMOF primitive cell cif ( NH2 and carboxyl group removed by Avogadro program and pymatgen script)
2x2x2 Supercell
Primitive Cell
Method
Avogadro Program을 사용해서 식별되는 모든 NH2를 H로 수동으로 바꿨으며, Ti와 Ti를 연결하는 링커 분자들 중 일부 분자들에 대해 카복실기 한 개를 제거하는 작업 수행
VESTA에서 시각화
VESTA에서 2x2x2 boundary 확장 및 슈퍼셀 시각화

## Slide 5
BAMOF semi optimized primitive cell cif ( optimized by Avogadro Program which uses UFF Force Field )
2x2x2 Supercell
Primitive Cell
Method
Avogadro Program을 사용해서 제작한 BAMOF를 세미 구조 최적화 (UFF Force Field사용)
VESTA에서 시각화
VESTA에서 2x2x2 boundary 확장 및 슈퍼셀 시각화

## Slide 6
DFT Convergence Test for “ecutwfc wavefunction cutoff energy” and “kpoint grids” by Quantum espresso
Kpoints grids
ecutwfc
1x1x1
2x2x2
3x3x3
1x1x1
대비
수렴 에너지
차이
(y축)
(kJ/mol)
Method
ecutwfc Convergence test
Basetemplate : https://github.com/dydtkddl/PSID_server_room/blob/main/qe/%5B00%5DBAMOF/02convergence_test_MIL125NH2/01ecut_wfc/00base_template.in
Kpoints Convergence test
Basetemplate : https://github.com/dydtkddl/PSID_server_room/blob/main/qe/%5B00%5DBAMOF/02convergence_test_MIL125NH2/06kpoints/00base_template.in

## Slide 7
MIL125-NH2 optimized primitive cell cif ( optimized by Quantum Espresso pw.x’s VC-relax and relax )
2x2x2 Supercell
Primitive Cell
Method
Avogadro로 최적화한 초기위치로 시작하여 QuantumEspresso로 Vc-relax및 relax최적화 진행.
input 구성 : https://github.com/dydtkddl/PSID_server_room/blob/main/qe/%5B00%5DBAMOF/05relaxation_MIL125NH2/smearing/input.in
VC-relax / Smearing / degauss 0.05

## Slide 8
BAMOF optimized primitive cell cif ( optimized by Quantum Espresso pw.x’s VC-relax and relax )
2x2x2 Supercell
Primitive Cell
Method
Avogadro로 최적화한 초기위치로 시작하여 QuantumEspresso로 Vc-relax및 relax최적화 진행.
input 구성 : https://github.com/dydtkddl/PSID_server_room/blob/main/qe/%5B00%5DBAMOF/04relaxation_BAMOF_1/05_SMEARING_AVO_OPT/fermi/input.in
VC-relax / Smearing / degauss 0.05

## Slide 9
BAMOF geometry optimize process video (VC-relax and Relax)
Method
Quantum Espresso 로 최적화하는 trajectory를 시각화.
output file을 trj xyz파일로 만드는 코드
https://github.com/dydtkddl/PSID_server_room/blob/main/qe/qe_crop_vc.py
시각화
OVITO 프로그램 사용

## Slide 10
MIL125-NH2 geometry optimize process video (VC-relax and Relax)
Method
Quantum Espresso 로 최적화하는 trajectory를 시각화.
output file을 trj xyz파일로 만드는 코드
https://github.com/dydtkddl/PSID_server_room/blob/main/qe/qe_crop_vc.py
시각화
OVITO 프로그램 사용

## Slide 11
MIL125NH2 scf calculation for DDEC charge analysis (PAW pseudo potential)
Method
David’s PAW pseudo potential 사용 : https://sites.google.com/site/dceresoli/pseudopotentials
convthr = 1e-8
smearing 적용
Output log analysis

## Slide 12
BAMOF scf calculation for DDEC charge analysis (PAW pseudo potential)
Method
David’s PAW pseudo potential 사용 : https://sites.google.com/site/dceresoli/pseudopotentials
convthr = 1e-8
smearing 적용
Output log analysis

## Slide 13
MIL125NH2 & BAMOF pp.x calculation to generate .cube that have electro density informations (very large file)
Method
pp.x program사용
3차원 큐브 파일 생성

## Slide 14
DDEC charge for BAMOF primitive cell
Method
chargemol.x 프로그램 사용 https://github.com/berquist/chargemol.git Quantum Espresso SCF계산 output기반으로 DDEC charge 계산
chargemol 인풋 https://github.com/dydtkddl/PSID_server_room/blob/main/qe/%5B00%5DBAMOF/06BAMOF_1_DDEC/03_DDEC_chargemol/David_Plot17_TI_core10/job_control.txt
시각화
Jmol 시각화 : JMOL 시각화 방법

## Slide 15
DDEC charge for MIL125-NH2 primitive cell
Method
chargemol.x 프로그램 사용 https://github.com/berquist/chargemol.git Quantum Espresso SCF계산 output기반으로 DDEC charge 계산
chargemol 인풋 https://github.com/dydtkddl/PSID_server_room/blob/main/qe/%5B00%5DBAMOF/07MIL125NH2_DDEC/03_chargemol/David_Plot17/job_control.txt
시각화
Jmol 시각화 : JMOL 시각화 방법